MIPOLAM ELEGANCE

MIPOLAM ELEGANCE is a monolayer homogeneous flooring with a high PVC content pressed in 2m sheets, with a thickness of 2mm and a weight of ≤ 2850g.

The non directional design with colour throughout the thickness integrates a 3D effect (transparent particles in pure PVC on all 33 references) and a matt finish.

This flooring is recommended for administrative buildings making skirtings easier, as well as angles and welding.

The flooring is equipped with Evercare™ the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. This Evercare™ treatment avoids staining of chemical products used in Healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics and does not require the application of acrylic polishes.

The flooring is composed of minimum 25% recycled content 100% controlled and is REACH compliant. It is 100% recyclable and 100% phthalates free.

This flooring is antistatic (<2kV), compliant to EN ISO 10581 with a binder content type I, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.

The product is non reactive to residual indentation with a value ≤ 0,02 mm.

The product emission rate of volatile organic compounds is <10 µg/m3 (TVOC after 28 days ISO 16000-6).