MIPOLAM ACTION

MIPOLAM® ACTION is a fully flexible compacted floorcovering in sheet, 2m wide, abrasion group T, providing excellent resistance to wear and tear in high traffic areas. Its weight is 2980 gr/sqm. It features a non-directional design incorporating coloured chips to ensure an even colour throughout the thickness.

This floorcovering is recommended for private and administrative buildings and thanks to its great flexibility it simplifies the installation of bend-up skirting, as well as angles and hot welding procedures.

Its surface is densely compacted for improved wear and ease of maintenance. It receives PUR Protect surface treatment with excellent cleaning characteristics, improved resistance to scratching and scuffing.

This floorcovering has extremely low VOC emissions, more than 40 times lower than the European standards ( <10 µg/m3 TVOC after 28 days ISO 16000-6).

This floorcovering is anti-static (<2kV) and resistant to the main chemical products used in healthcare and is non-reactive to residual indentation with a value ≤ 0,04 mm (EN 433).

MIPOLAM® ACTION is available in 22 relaxing colours.

As part of our sustainable development policy, this product is manufactured in a plant certified with highest quality standards iSO 9001 and environmental standards iSO 14 001.