Creation 70 Connect is a synthetic, decorative, flexible, antistatic, abrasion group T floorcoverings available in tiles. It consists in a 0,70mm thick transparent wear layer, a design film, a calendared layer and a PVC compact sublayer reinforced with fibers. The overall thickness is 5mm.

They benefit from a PUR+ Matt surface treatment, making maintenance easier and eliminating the need for initial polishes.

Creation 70 Connect is an interlocking floorcovering, resistant to use (commercial / industrial use) of 34 / 43 according to EN-ISO 10874 and has Bfl-s1 class for smoke emission according to EN 13501-1.

Creation 70 Connect is compatible with occasional traffic (1 time per day) of manual pallet truck with a total loaded weight up to 250kg.

Creation 70 Connect is made with phthalate free plasticizers, except recycled content. It is 100% recyclable and made with 55% of recycled content. It is REACH compliant. The product emission rate of organic compounds is < 10µg/m3 (TVOC <28 days – ISO 16000-6).