MARMORETTE SPORT

MARMORETTE SPORT is a two layer calendered linoleum compact floorcovering in sheet, 2m wide.

Its weight is 3800gr/sqm in 3,2mm.

It features a marbled design.

It is composed of 98% natural materials (bio-based and mineral): linseed oil, wood flour, resins, cork, minerals and jute fabric, among which 76% are rapidly renewable.

The flooring is 100% recyclable, is composed of minimum 25% recycled content and up to 40% recycled content, 100% controlled, is REACH compliant, rated Cfl-s1 for fire resistance and is antistatic.

The product also benefits from international certifications such as Floorscore and Blue Angel (emissions).

Designed and manufactured in a sustainable way in a plant awarded with ISO 9001 (quality), ISO 14001 (environment) and ISO 50001 (energy) certifications, the flooring is certified “Cradle to Cradle Silver". Its Environmental Performance Declaration (EPD) certified by an external laboratory, indicates carbon neutrality during the first stages of its life cycle ("from cradle to gate").