MIPOLAM ACCORD

MIPOLAM ACCORD is a monolayer homogeneous flooring with high PVC content calendered and pressed in 2m sheets, with a thickness of 2mm and a weight of ≤ 2790g.

The semi-directional design with colour throughout the thickness is available in 28 references presenting a nice matt finish.

This flooring is recommended for collective buildings making skirtings easier, as well as angles and welding.

The flooring is equipped with Evercare TM the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. This Evercare TM avoids staining of chemical products used in Healthcare like betadine, eosin or anti-bacterial hand gel and increases the durability of the flooring.

This treatment has excellent maintenance characteristics and does not require the application of acrylic polishes

The flooring is composed of minimum 25% recycled content 100% controlled and is REACH compliant.

According to ISO 21702, Mipolam Accord has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2h00.

According to ISO 22196, Mipolam Accord has anti bacterial activity againt E. coli, S. aureus and  MRSA of 99% after 24h00.

On demand, MIPOLAM ACCORD is available with phthalate free plasticizer.

This flooring is anti-static (<2kV).The product is non-reactive to residual indentation with a value ≤ 0,02 mm to 150 minutes respecting EN ISO 24343-1 (EN 433).

The flooring is compliant with EN ISO 10581 norm, has a binder content type I, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.

The product emission rate of volatile organic compounds is <10 µg/m3 (TVOC after 28 days ISO 16000-6), is 100% phthalates free and 100% recyclable.