PRODUCT DESCRIPTION

MIPOLAM BIOCONTROL EL5

MIPOLAM BIOCONTROL EL5 is a conductive flexible homogeneous vinyl floorcovering available in sheet.

The 2 mm homogeneous material incorporates carbon encapsulated granules throughout its full thickness. It has a conductive backing to ensure optimal and consistent conductive properties throughout its full life expectancy.

This floorcovering has a conductive surface treatment which avoids stain of chemical products increasing durability of the flooring.

MIPOLAM BIOCONTROL EL5 acts as a continuous conductive floor. It has permanent antistatic properties (< 100 V). The product has to be grounded with an ESD copper strip (cf. finishes) to meets its full performance. No need to lay with conductive glue.

The product is non-reactive to residual indentation with a value ≤ 0,02 mm (EN ISO 24343-1)

The flooring complies with the EN ISO 10874 (34-43) offering a binder content type II, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.

The product is non-emissive of volatile organic compounds with <10 µg/m3 (TVOC after 28 days ISO 16000-6).

Mipolam Biocontrol EL5 is conform to IEC 61340-5.1 and ESD 2020 and is Fraunhofer ISO 5 certified for particles emission.