MIPOLAM BIOCONTROL CLEAN

MIPOLAM BIOCONTROL CLEAN is fully flexible homogeneous compacted floorcovering in sheet, 2m wide, providing excellent resistance to wear and tear in high traffic areas. It has therefore has a high resistance to heavy loads.

Certified ISO3, it is particularly recommended for use in clean rooms.

MIPOLAM BIOCONTROL CLEAN has an exclusive surface treatment offering the best chemical resistance to the main products used in healthcare environment as Betadine, eosin, hydro alcoholic solutions, making the maintenance easy and long lasting the flooring.

This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

According to ISO 21702, MIPOLAM BIOCONTROL CLEAN has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,7% after 2 hours, and 99,9% after 5 hours.

According to ISO 22196, MIPOLAM BIOCONTROL CLEAN has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

Its suitability for nuclear decontamination according to the ISO 8690 standard is excellent.

Bacteriostatic, it prevents the development of micro-organisms in the soil.

It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio  accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant. It is 100% phthalates free and recyclable.
Its VOC emissions after 28 days (ISO 16000-6) are below detection levels (<10 μg / m3) and this product is classified A + (the best class).

The flooring is antistatic (<2kV), its residual indentation is ≈ 0.02 mm.

The flooring complies with the EN ISO 10581 norm, has a binder content Type I and is suitable for heavy duty traffic areas and Bfl-s1 fire resistance.

As part of our sustainable development policy, this product is manufactured in the first floor covering plant awarded with the triple certification: ISO 9001 (quality),

ISO 14 001 (environment) and OHSaS 18001 (safety).