CREATION EVO is a decorative and flexible floorcovering available in tile or plank, with beveled edges. It consists in a polymer blend without PVC and technical mineral filler. The overall thickness is 2 mm.

They benefit from a cross-linked polyurethane surface treatment, making maintenance easier and eliminating the need for initial polishes.

CREATION EVO is a glued floorcovering, resistant to use (commercial and industrial use) of 34 / 43 according to EN-ISO 10874 and has Bfl -s1 class for smoke emission on concrete subfloor according to EN 13501-1.

CREATION EVO is phthalate free and is blue angel certified. It is 100% recyclable and made with 25% of recycled content. It is 100% compliant with REACH. The product emission rate of organic compounds is < 10 micrograms/m3 (TVOC <28 days – ISO 16000-6).