GTI EL5 CLEANTECH is a multi-layered looselay vinyl tile, 6 mm thick, reinforced with 2 glass fiber grids.

GTI EL5 CLEANTECH tiles are available in square format with welded joints for clean environments and watertight systems requirements.

GTI EL5 CLEANTECH wearlayer is 2 mm vinyl homogeneous manufactured with continuous high pressure process, abrasion group P.

It complies with EN 649 and offers an outstanding resistance to traffic.

This floorcovering is treated with Evercare™ technology: the latest improvements in polyurethane surface treatment obtained by UV laser cross-linking. Evercare™ offers easy maintenance and avoids staining of chemical products used in industry and healthcare, like betadine, eosin, anti-bacterial hand gel and also bio-
decontamination procedures. This treatment has excellent maintenance characteristics; it requires no wax for life!

The carbon encapsulated granules throughout its full thickness and the conductive backing and conductive surface treatment ensure optimal and consistent conductive properties throughout its full life expectancy. GTI EL5 CLEANTECH acts as a continuous conductive: 5 x 104 ≤ Rt ≤ 106 (EN1081 – IEC61340-4-1≤108).

It has permanent antistatic properties: <2000V (EN1815), <100 V (IEC61340-4-5).

The product is non-emissive of volatile organic compounds with <10 μg/m3 (TVOC after 28 days ISO 16000-6).

Complementary finishes:

GTI EL5 ACCESS (access ramp), GTI EL5 CORNER (corner finishes), GTI EL5
CONTROL coving (COVING / COVING CORNER IN and COVING CORNER OUT) and conductive welding rods (GTI EL5 CONTROL WELDING RODS).