GUIDE SPECIFICATION

096519- Resilient Tile Flooring including Solid Vinyl Floor Tile

(Section 096519.23 – Resilient / Vinyl Tile Flooring)

Gerflor Creation Connect Resilient Tile Flooring

This is an editable document for preparing project specifications for Gerflor Creation Connect Resilient Tile Flooring with PUR+Matte.

How to use this Guide Specification:

This is an “edit-out” document with specification language for several project options.              Select appropriate text based on the project requirements and delete (edit-out) all other text.

- Specifier notes are shown in blue like this: Editor Notes

- Locations where language for Project-specific requirements is to be inserted or selected are indicated like this: [insert] or [select text].

- Finally, remove Editor Notes and any unused optional text in the final version of the specification document.

This document contains trademarks owned by Gerflor including PUR+Matte.

Gerflor USA, 750 Veterans Parkway, Bolingbrook, IL 60440 USA. Phone: (877) 437-3567.                E-mail: info@gerflorusa.com. Website: gerflorusa.com

SECTION 096519.23 – Resilient / Vinyl Tile Flooring

- GENERAL

      - SUMMARY

        - Section Includes: Resilient vinyl tile flooring

      - ACTION SUBMITTALS

        - Product Data: For each type of product indicated.

        - Manufacturer Certifications:

          - Provide certification that accurately identifies the Original Equipment Manufacturer (OEM) of flooring furnished for this project including manufacturer’s name, address and factory location.

            - Suppliers of Private-Label flooring for this project must identify themselves as such and fully disclose the OEM information listed above.

            - All “manufacturer” requirements in these specifications must be complied with by the OEM, including warranties, certifications, qualifications, product data, test results, environmental requirements, performance data, etc.

          - Provide ISO 9001 certification for the OEM of the specified products.

          - Provide ISO 14001 certification for the OEM of the specified products.

        - Shop Drawings: Showing installation details and locations of borders, patterns, locations of any floor inserts and any seams.

        - Samples:

          - Manufacturer's color chart for selection of available floors

          - Product samples:

            - Samples to be a minimum of 10”x10”

      - INFORMATIONAL SUBMITTALS

        - Qualification Data:

          - For a qualified resilient flooring Manufacturer.

          - For a qualified resilient flooring Installer.

      - CLOSEOUT SUBMITTALS

        - Submit three copies of the following:

          - Manufacturer maintenance instructions.

          - Manufacturer material warranty.

      - QUALITY ASSURANCE

        - Manufacturer Qualifications:

          - ISO 9001 Certified.

          - ISO 14001 Certified.

          - At least ten years active experience in the manufacture and marketing of commercial resilient flooring.

          - A provider of authorized installer training.

        - Installer Qualifications:

          - At least five years experience in the installation of resilient flooring.

          - Experience on at least five projects of similar size, type and complexity as this project.

          - Employer of workers for this Project who are competent in techniques required by manufacturer for resilient flooring installation indicated.

        - Fire Test Characteristics: As determined by testing identical products according to ASTM E 648, Class 1, by a qualified testing agency acceptable to authorities having jurisdiction.

      - DELIVERY, STORAGE, AND HANDLING

        - Store flooring and installation materials in protected dry spaces, with ambient temperatures maintained within range recommended by manufacturer, but not less than 55 deg F (13 deg C) nor more than 85 deg F (29 deg C).

        - Store the indoor resilient luxury vinyl tiles (LVT) boxes on a smooth flat surface immediately upon delivery to Project.

      - FIELD CONDITIONS

        - Product Installation:

          - Maintain temperatures during installation within range recommended by manufacturer, but not less than 65 deg F (18 deg C) in spaces to receive flooring one week before installation, during installation, and maintain thereafter installation.

          - After installation, maintain temperatures within range recommended by manufacturer, but not less than 65 deg F (18 deg C) or more than 85 deg F (29 deg C).

          - Prohibit traffic during flooring installation.

          - Refer to the adhesive technical data sheet for appropriate time for traffic after installation.

        - Install flooring only after other finishing work, including painting and overhead work, has been completed.

      - WARRANTY

        - Manufacturer warrants that flooring products are free from manufacturing defects.  Refer to product-specific warranty document for additional detail and warranty period.

          - Material warranty must be direct from the product manufacturer.

          - Material warranties from separate or third-party insurance providers are not valid.

          - Material warranties from private label distributors are not valid.

          - Failures include the following:

            - Material manufacturing defects.

          - Warranty Period:

            - For materials: 10 years from date of Substantial Completion.

      - ENVIRONMENT AND INDOOR AIR QUALITY

        - LEED® Documentation:

          - LEED v4 MR Credit, Building Product Disclosure & Optimization, Sourcing of Raw Materials: For products having recycled content, indicate percentage by weight of post-consumer and pre-consumer recycled content.

          - LEED v4 EQ Credits: For adhesives and flooring, including a statement of VOC content, FloorScore® certified.

        - Indoor Air Quality Certification:

          - Flooring products must be FloorScore® Certified.

            - FloorScore® certification proves compliance with the volatile organic compound emissions criteria of the California Section 01350 standard.

            - FloorScore® certification proves compliance with the testing and product requirements of the California Department of Health Services “Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers.”

            - FloorScore® documentation must include certificate number for specified product.

        - Manufacturer Certification of Environmental Procedures:

          - Original Equipment Manufacturer’s (OEM) ISO 14001 Certification

      - COORDINATION

        - Coordinate layout and installation of flooring with other equipment.

- PRODUCTS

      - COMMERCIAL RESILIENT / VINYL TILE FLOORING

- Editor Note: Select specific Creation Connect  design and description where indicated.

        - Basis-of-Design Manufacture: Subject to compliance with requirements, provide Creation Connect with PUR+Matte.

- Gerflor’s Creation Connect is a 27.6” x 27.6” with 10 dovetails per side resilient multilayered interlocking tile.  Its total thickness is 5mm printed design protected by a 28mil (0.70mm) thick transparent wear layer, a compact backing made of recycled and cork materials providing sound management properties and PUR+Matte  surface treatment.

- Flooring installed with full-spread standard adhesive.

Editor Note:

Select one of the following 3 paragraphs to address consideration of additional manufactures:

If no substitutions will be accepted:

        - Substitution Limitations:

          - No substitutions.

If products from other manufacturers will be considered, insert the manufacture’s name and the product name and/or model number:

        - Other Manufactures: Subject to compliance with all the requirements of this specification, provide products by one of the following:

          - [Insert flooring manufacturer name] : [Insert flooring product name/model].

If other manufacturers are allowed to submit requests for approval prior to bid:

        - Substitution Limitations:

          - All other manufacturers: Submit formal substitution request prior to bid in accordance with Section 012500 - "Substitution Procedures”.

          - Approval by Architect of other manufacturers does not relieve Contractor of responsibility to provide products which comply with all requirements of this specification.

        - Product Description:  Resilient / Vinyl Tile flooring as per ASTM F1700.

          - Overall Thickness: Not less than 3/16” (5 mm)

          - Wear-Layer Thickness: Not less than 028 mil (0.70 mm)

          - Adhesive Method:

            - Full-spread adhesive to completely adhere flooring to substrate.

            - Complete adhesive coverage to eliminate the possibility of gaps or space between the slab and flooring material where moisture could accumulate and create an environment conducive to mold growth.

            - Flooring to be adhered to the concrete slab in all locations eliminating the possibility of gaps or buckling forming caused by the floor shifting, moving or by rolling loads displacing it.

          - 100% REACH Compliant.

          - Applied Finish: Manufacturer's, factory-applied, permanent, UV-cured.

            - PUR+Matte

          - Tile size: 27.6” x 27.6”

          - Color and Pattern:

- a. As selected by Owner from manufacturer’s standard colors and patterns.

        - Performance Criteria:

          - ASTM F1700 for vinyl tile floor covering

            - Provide test certificate to show compliance with ASTM F1700

      - ACCESSORIES

        - Trowelable Leveling and Patching Compound: Latex-modified, hydraulic-cement-based moisture insensitive formulation approved by the flooring manufacturer.

        - Adhesives: Acrylic types recommended by flooring manufacturer for substrate and conditions indicated.

            - Basis-of-Design Product: Gerfix TPS+, Gerfix 100, T-111, Gerfix LVT & Plank Spray.

            - Coverage Type: Refer to manufacturer’s installation instructions.

            - Adhesives Available for “No Down Time” / Immediate Traffic Installations.

            - Adhesive available for 100% RH Slab Moisture Installations with no vapor retarder needed beneath the concrete.

- EXECUTION

      - EXAMINATION

        - Verify the Following:

          - The area in which the indoor resilient tile flooring will be installed is dry, weather-tight and in compliance with specified requirements.

          - Permanent heat, lighting and ventilation systems are installed and operable.

          - Other work, including overhead work, that could cause damage, dirt, dust or otherwise interrupt installation has been completed or suspended.

          - No foreign materials or objects are present on the substrate and that it is clean, porous, and ready for preparation and installation.

          - Tests to verify that the moisture vapor emission rate or substrate relative humidity is within the specified ranges if applicable.

          - The concrete slab surface pH level is within the specified range.

          - The concrete slab surface deviation is no greater than 3/16 inch within 10 feet as described in ASTM F710.

          - The concrete slab complies with ACI 302.2R for concrete design including use of a low-permeance vapor barrier directly beneath the concrete subfloor with sealed penetrations.

      - PREPARATION

        - Prepare substrates according to manufacturer's written recommendations to ensure proper adhesion of resilient flooring system.

        - Concrete Substrates: Prepare according to ASTM F710.

          - Verify that substrates are dry and free of sealers, curing compounds and other additives. Remove coatings and other substances that are incompatible with adhesives using mechanical methods to create porosity as recommended by manufacturer.

          - Alkalinity Testing: Proceed with installation if the pH readings are within the specifications given by the adhesive manufacturer.

        - Moisture Testing: Moisture Testing: If applicable, perform ASTM F 2170 relative humidity test and proceed with installation only after substrates are below relative humidity of the selected adhesive.  Or perform ASTM F1869 calcium chloride test and proceed with installation only after substrates are below the maximum moisture-vapor-emission rate of the selected adhesive. Where only one test protocol can be performed, ASTM F2170 is preferred.

        - Use trowelable concrete based leveling and patching compound with the same moisture vapor tolerance as the adhesive to fill depressions, holes, and other irregularities in substrate. For dormant cracks and saw cuts refer to manufacturer’s installation instructions.

        - Place flooring and installation materials into spaces where they will be installed at least 48 hours before installation. Install flooring materials only after they have reached the same temperature as space where they are to be installed.

        - Mechanically prepare the surface of the concrete slab per ASTM F710.

        - Sweep and then vacuum substrates immediately before installation. After cleaning, examine substrate for moisture, alkaline salts, grit, dust or other contamination. Proceed with installation only after unsatisfactory conditions have been corrected.

      - VINYL TILE FLOORING INSTALLATION

        - General:

          - Comply with resilient tile flooring manufacturer's installation instructions.

          - Take necessary precautions to minimize noise, odors, dust and inconvenience during installation.

          - Fit flooring neatly and tightly to vertical surfaces, equipment anchors, floor outlets, and other interruptions of floor surface.

          - Extend flooring into toe spaces, door reveals, closets, and similar openings unless otherwise indicated.

        - Lay out flooring per manufacturer’s recommendations.

        - Adhered Flooring: Attach products to substrates using a full spread of adhesive applied to substrate to comply with adhesive and flooring manufacturer instructions.

      - CLEANING AND PROTECTION

        - Perform cleaning 72 hours after completing resilient flooring installation:

          - Remove marks from flooring surfaces.

          - Sweep and then vacuum flooring.

          - Damp-mop flooring with pH neutral cleaner to remove soiling.

        - Protect flooring from abrasions, indentations, and other damage from subsequent operations and placement of equipment, during remainder of construction period.

END OF SECTION