TARALAY MILLENIUM ACOUSTIC is a multilayered vinyl floorcovering available in 2m wide sheet.

The product comprises a 1 mm thick coated wear layer, made of pure vinyl, coloured throughout its thickness (no transparent wear layer and no filler). Its complete thickness is 3.4 mm.

It contains a Very High Density (VHD) foam backing and is reinforced with 2 fibre glass grids which yields a 17dB sound insulation rating and a resistance to indentation of 0.07 mm.

This flooring is protected by the surface treatment, Protecsol® mat, with a minimum thickness of 13µm, ensuring easy maintenance and no required polish for the entire lifetime of the product.

According to ISO 21702, TARALAY MILLENIUM ACOUSTIC has anti viral activity against Human Coronaviruses : it reduces the number of virus by 99,37% after 2h00.

According to ISO 22196, it has anti bacterial activity against E. coli, S. aureus and  MRSA of 99% after 24h00.

It is composed of 50% mineral and inexhaustible materials. It does not contain any heavy metals or CMR 1&2 components, it is phthalate-free and 100% compliant with REACH. The product emission rate of volatile organic compounds is <10µg/m³ (TVOC after 28 days ISO 16000-6). It is 100% recyclable.