CREATION 40 ZEN is an acoustic and decorative floor, in PVC multilayers reinforced with a fiber veil, available in tile and plank format, with 4 beveled edges.

It has antistatic abrasion group T, and R10 antislip performance.

The overall thickness is 3.60 mm, and the product has 0.40 mm transparent wearlayer.

The high density foam provides good indentation resistance of 0.12 mm (average mesure) and high acoustic insulation level (-20 dB)

It  benefits from a cross-linked polyurethane surface treatment (ProtecshieldTM), making maintenance easier and prevent from micro scratches.

CREATION 40 ZEN has a European class (residential / commercial) 23/32 according to EN-ISO 10874 and has Bfl-s1 class for smoke emission according to EN 13501-1.

CREATION 40 ZEN is a looselay product, maintained with tackifier.

This installation allows, among other things, an installation on asbestos-contaminated support, and is removable

CREATION 40 ZEN is made with phthalate free plasticizers. It is 100% recyclable and 100% compliant with REACH. The product emission rate of organic compounds is < 10µg/m3 (TVOC <28 days – ISO 16000-6).

CREATION 40 ZEN is made in France