Mipolam Comet

MIPOLAM COMET is a vinyl flooring homogeneous pressed in 2m sheets, with a thickness of 2mm and a weight ≤ 2950g.

The timeless design with colour throughout the thickness is available in 26 references presenting a nice matt finish.

This flooring is suitable for medium to high traffic areas, and facilitates floor–wall junctions, angles and welding treatments.

The flooring is equipped with PUR+, surface treatment offering an excellent chemical resistance to the main products used in healthcare environment as Betadine, eosin, hydro alcoholic solutions, making the maintenance easy and long lasting the flooring. This treatment avoids applying any acrylic emulsion throughout the lifetime of the product.

It is composed of 57% natural content (mineral + recycled). It is free of formaldehyde, heavy metals and CMR 1 & 2 or vPvB (very persistent and very bio accumulative) or PBT (persistent, bio-accumulative and toxic) and is REACH compliant. It is phthalates free and 100% recyclable.

According to ISO 22196, Mipolam Comet has anti bacterial activity against E. coli, and  MRSA of 99% after 24h00.

COV emissions after 28 days (ISO 16000-6) are below detection levels with <10 μg / m3.

The flooring is antistatic (<2kV), its residual indentation is ≤ 0.10 mm.

The flooring is compliant with EN ISO 10581 norm, has a binder content type I, is suitable for heavy duty traffic areas and has Bfl-s1 fire resistance.