TARALAY INITIAL ACOUSTIC

TARALAY INITIAL ACOUSTIC is an acoustic multi-layered vinyl floorcovering, available in 2m wide sheet, with a group T wear rating.

The product comprises a foam backing reinforced with a glass fibre and a printed design that is protected by a transparent wear layer (0.65 mm thick). It offers 19 dB sound insulation and an indentation resistance of 0.10 mm.

It is treated with Protecsol®, a UV cured surface treatment, which facilitates ease of maintenance and eliminates permanently the need for acrylic emulsion (metallisation).

It does not contain any heavy metals or CMR 1&2 and is 100% compliant with REACH. The products emission rate of volatile organic compounds is < 10 µg/m3 (TVOC after 28 days – ISO 16000-6). It is 100% recyclable.

Regarding norm ISO 22196, the product will provide antibacterial activity against E.coli, S.aureus and MRSA bacteria by reducing the number of virus by 99% after 24 hours.

Regarding norm ISO 21702, the product will provide antiviral activity against human Coronavirus by reducing the number of virus by 99,3% after 2 hours.

Modèle de descriptif	gerflor.fr