VIRTUO 55 DRYBACK is a decorative LVT flooring, available in tiles and planks, with beveled edges. It is 2.5 mm thick, and the wear layer is 0,5 mm.

It is made with phthalate free plasticizers. It is 100% recyclable and made with up to 19% of recycled content. It is 100% compliant with REACH. The product emission rate of volatile organic compounds is < 10µg/m3 (TVOC <28 days – ISO 16000-6).

VIRTUO 55 DRYBACK is an LVT PVC flooring covering made by hot press or calandering. Intend of is housing. They are presented in the form of tiles and plankes glued on the surface.

They are made of a wear layer applied on a high quality a high-definition printed decorative film to offer maximum variety in the design and a backing lawer in contact with the substract.

This product is dedicated to light traffic 33/42 according the En ISO 10874. It Bfl-S1 approved according to the EN 13501-1. TVOC after 28 days is <10 µg/m3 –ISO16000-6.