GTI EL5 CONNECT is a multi-layered, looselay vinyl tile with a thickness of 6 mm, reinforced by two glass fiber grids. These tiles can be installed using an interlocking system with dovetails.

The wear layer of GTI EL5 CONNECT is a 2 mm homogeneous vinyl, manufactured through a continuous high-pressure process, classified under abrasion group P. Compliant with EN 649 standards, it offers exceptional resistance to heavy traffic.

This floor covering is treated with Evercare™ technology, incorporating the latest advancements in polyurethane surface treatment achieved through UV laser cross-linking. Evercare™ ensures easy maintenance and prevents staining from various chemicals used in industrial and healthcare settings, such as betadine, eosin, antibacterial hand gel, and bio-decontamination agents. This treatment boasts excellent maintenance characteristics and requires no waxing for its entire lifespan.

The carbon encapsulated granules throughout its full thickness, along with the conductive backing and surface treatment, guarantee optimal and consistent conductive properties throughout its lifespan. GTI EL5 CONNECT functions as a continuous conductive material: 5×104≤Rt≤106 (EN1081 – IEC61340-4-1 ≤ 108).

It possesses permanent antistatic properties: <2000V (EN1815), <100V (IEC61340-4-5).

Additionally, the product is non-emissive of volatile organic compounds, with levels <10 μg/m³ (TVOC after 28 days, ISO 16000-6).