GTI MAX CLEANTECH is a multi-layered, loose-lay vinyl tile with a thickness of 6 mm, reinforced by two glass fiber grids. These tiles are available in a square format with welded joints, making them ideal for clean environments and watertight system requirements.

GTI MAX CLEANTECH features a 2 mm homogeneous vinyl wear layer, manufactured through a continuous high-pressure process offering exceptional resistance to heavy traffic and static loads (CSTB classification for industrial floors R2 and UPEC classification U4P4S).

GTI MAX CLEANTECH is treated with Polyurethane (PUR) surface treatment, ensuring easy maintenance and preventing staining from various chemicals used in industrial settings. This treatment boasts excellent maintenance characteristics and requires no waxing for its entire lifespan.

GTI MAX CLEANTECH possesses permanent antistatic properties: <2000V (EN1815).

GTI MAX CLEANTECH is non-emissive of volatile organic compounds, with levels <10 μg/m³ (TVOC after 28 days, ISO 16000-6).