GUIDE SPECIFICATION

096519- Resilient Tile Flooring

(Section 096519.13 – Conductive Resilient Tile Flooring)

Gerflor® GTI EL5 Connect  Conductive Resilient Tile Flooring

This is an editable document for preparing project specifications for Gerflor GTI EL5 Connect Tile Flooring.

How to use this Guide Specification:

This is an “edit-out” document with specification language for several project options.              Select appropriate text based on the project requirements and delete (edit-out) all other text.

- Specifier notes are shown in blue like this: Editor Notes

- Locations where language for Project-specific requirements is to be inserted or selected are indicated like this: [insert] or [select text].

- Finally, remove Editor Notes and any unused optional text in the final version of the specification document.

This document contains trademarks owned by Gerflor including GTI EL5 Connect, Gerfix, Evercare.

Gerflor USA, 750 Veterans Parkway, Bolingbrook, IL 60440USA. Phone: (877) 437-3567.                E-mail: info@gerflorusa.com. Website: gerflorusa.com

SECTION 096519.13 – Conductive Resilient Tile Flooring

- GENERAL

      - SUMMARY

        - Section Includes: Conduct Resilient Tile Flooring

      - ACTION SUBMITTALS

        - Product Data: For each type of product indicated.

        - Manufacturer Certifications:

          - Provide certification that accurately identifies the Original Equipment Manufacturer (OEM) of flooring furnished for this project including manufacturer’s name, address and factory location.

            - Suppliers of Private-Label flooring for this project must identify themselves as such and fully disclose the OEM information listed above.

            - All “manufacturer” requirements in these specifications must be complied with by the OEM, including warranties, certifications, qualifications, product data, test results, environmental requirements, performance data, etc.

          - Provide ISO 9001 certification for the OEM of the specified products.

          - Provide ISO 14001 certification for the OEM of the specified products.

          - Provide ISO 50001 certification for the OEM of the specified products.

        - Shop Drawings: Showing installation details and locations of borders, patterns, locations of floor inserts and seams.

        - Samples:

          - Manufacturer's color chart for selection of available floors

          - Product samples:

            - Samples to be a minimum of 6’’ x 9’’

      - INFORMATIONAL SUBMITTALS

        - Qualification Data:

          - For a qualified resilient flooring Manufacturer.

          - For a qualified resilient flooring Installer.

      - CLOSEOUT SUBMITTALS

        - Submit three copies of the following:

          - Manufacturer maintenance instructions.

          - Manufacturer material warranty.

      - QUALITY ASSURANCE

        - Manufacturer Qualifications:

          - ISO 9001 Certified.

          - ISO 14001 Certified.

          - ISO 50001 Certified.

          - At least ten years active experience in the manufacture and marketing of commercial resilient flooring.

          - A provider of authorized installer training.

        - Installer Qualifications:

          - At least five years experience in the installation of resilient flooring.

          - Experience on at least five projects of similar size, type and complexity as this project.

          - Employer of workers for this Project who are competent in techniques required by manufacturer for resilient flooring installation indicated.

        - Fire Test Characteristics: As determined by testing identical products according to ASTM E648, Class 1, by a qualified testing agency acceptable to authorities having jurisdiction.

      - DELIVERY, STORAGE, AND HANDLING

        - Store static-control resilient flooring and installation materials in dry spaces protected from the weather, with ambient temperatures maintained within range recommended by manufacturer but not less than 55° F (13° C) or more than 85° F (29° C).

          - Store the indoor tiles (boxes) on a smooth flat surface immediately upon delivery to project.

      - FIELD CONDITIONS

        - Product Installation:

          - Maintain temperatures during installation within range recommended by manufacturer, but not less than 65° F (18° C) in spaces to receive flooring one week before installation, during installation, and maintenance thereafter installation.

          - After installation, maintain temperatures within range recommended by manufacturer, but not less than 65° F (18° C) or more than 85° F (29° C).

          - Prohibit traffic during flooring installation.

          - Refer to the adhesive technical datasheet for appropriate time for traffic after installation.

        - Install static-control resilient flooring only after other finishing work, including painting and overhead work, has been completed.

      - WARRANTY

        - Manufacturer warrants that flooring products are free from manufacturing defects.  Refer to product-specific warranty document for additional detail and warranty period.

          - Material warranty must be direct from the product manufacturer.

          - Material warranties from separate or third-party insurance providers are not valid.

          - Material warranties from private label distributors are not valid.

          - Failures include the following:

            - Material manufacturing defects.

          - Warranty Period:

            - For materials: 10 years from date of Substantial Completion.

      - ENVIRONMENT AND INDOOR AIR QUALITY

        - LEED® Documentation:

          - LEED v5 MR Credit, Building Product Disclosure & Optimization, Environmental Product Declaration: Supply at minimum an industry-wide Environmental Product Declaration (EPD)

          - LEED v5 MR Credit, Building Product Disclosure & Optimization, Sourcing of Raw Materials: For products having recycled content, indicate percentage by weight of post-consumer and pre-consumer recycled content.

          - LEED v5 EQ Credits: For adhesives and flooring, including a statement of VOC content, FloorScore® certified.

        - Indoor Air Quality Certification:

          - Flooring products must be FloorScore® Certified.

            - FloorScore® certification proves compliance with the volatile organic compound emissions criteria of the California Section 01350 standard.

            - FloorScore® certification proves compliance with the testing and product requirements of the California Department of Health Services “Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers.”

            - FloorScore® documentation must include certificate number for specified product.

        - Manufacturer Certification of Environmental Procedures:

          - Original Equipment Manufacturer’s (OEM) ISO 14001 Certification

        - Manufacturer’s Certification to Inhibit the Spread of Bacteria

          - Product certified ISO 22196 compliant to inhibit the spread of bacteria at 99.9%

      - COORDINATION

        - Coordinate layout and installation of flooring with other equipment.

- PRODUCTS

      - COMMERCIAL TILE VINYL FLOORING

- Editor Note: Select specific GTI EL5 Connect design and description where indicated.

- Basis-of-Design Manufacture: Subject to compliance with requirements, provide Gerflor GTI EL5 Connect  [insert design] a 6mm thick, homogenous surface with conductive backing and surface ensures optimal and consistent conductive properties with Evercare® surface treatment.

- Editor Note: Select one of the following 3 paragraphs to address consideration of additional manufactures:

If no substitutions will be accepted:

        - Substitution Limitations:

          - No substitutions.

If products from other manufacturers will be considered, insert the manufacture’s name and the product name and/or model number:

        - Other Manufactures: Subject to compliance with all the requirements of this specification, provide products by one of the following:

          - [Insert flooring manufacturer name] : [Insert flooring product name/model].

If other manufacturers are allowed to submit requests for approval prior to bid:

        - Substitution Limitations:

          - All other manufacturers: Submit formal substitution request prior to bid in accordance with Section 012500 - "Substitution Procedures”.

          - Approval by Architect of other manufacturers does not relieve Contractor of responsibility to provide products which comply with all requirements of this specification.

        - Product Description: Conductive resilient tile floor covering complying with ASTM F1700.

          - Overall Thickness: Not less than 6mm

          - Max static load limit must exceed ASTM F970.

          - Adhesive Method: Refer to manufacturer's installation instructions to ensure proper installation and performance.

          - Bacteriostatic Performance: ISO 22196 compliant.

          - 100% REACH Compliant.

          - Applied Finish: Manufacturer's, factory-applied, permanent, laser and UV-cured.

            - No-Wax finish: Published product literature identifying factory UV-cured applied finish.

            - Basis-of-Design Product: Evercare®®

          - Field-Applied Finishes: None required and not allowed.

          - Tile Size:

            - Tile:  25” x 25”

          - Color and Pattern:

            - As selected by Owner from manufacturer's standard colors and patterns.

        - Performance Criteria:

          - Meets requirements for Classification standards ANSI/ESD 20.20 and IEC 61340-5-1

      - ACCESSORIES

        - Trowelable Leveling and Patching Compound: Latex-modified, hydraulic-cement-based moisture insensitive formulation approved by the flooring manufacturer.

        - Adhesives: Water-resistant type recommended by flooring manufacturer for substrate and conditions indicated.

            - Basis-of-Design Product: Gerflor Gerfix TPS+, Gerflor Spray Adhesive, Gerfix 196.

            - Coverage Type: grid pattern to adhere floor to substrate.

            - Adhesives available for “No Down Time” / Immediate Traffic Installations.

            - Adhesive available for 98% RH Slab Moisture Installations.

        - Copper Strip: Leads the electrostatic charge to the ground points

            - Basis-of-Design Product: Copper Strip

            - Width:  10 mm

            - Thickness: 0.08 mm

Specific Rheostat:  0,01693-0,017241 Ωmm²/m

            - GTI EL5 tiles must be grounded every 400 sq ft

- EXECUTION

      - EXAMINATION

        - Verify the Following:

          - The area in which the indoor resilient flooring will be installed is dry, weather-tight and in compliance with specified requirements.

          - Permanent heat, lighting and ventilation systems are installed and operable.

          - Other work, including overhead work, that could cause damage, dirt, dust or otherwise interrupt installation has been completed or suspended.

          - No foreign materials or objects are present on the substrate, and it is clean, porous, and ready for preparation and installation.

          - Tests to verify that the moisture vapor emission rate or substrate relative humidity is within the specified ranges if applicable.

          - The concrete slab surface pH level is within the specified range.

          - The concrete slab surface deviation is no greater than 3/16 inch within 10 feet as described in ASTM F710.

          - The concrete slab complies with ACI 302.2R for concrete design including use of a low-permeance vapor barrier directly beneath the concrete subfloor with sealed penetrations.

      - PREPARATION

        - Prepare substrates according to manufacturer's written recommendations to ensure proper adhesion of resilient flooring system.

        - Concrete Substrates: Prepare according to ASTM F710.

          - Verify that substrates are dry and free of sealers, curing compounds and other additives. Remove coatings and other substances that are incompatible with adhesives using mechanical methods to create porosity as recommended by manufacturer.

          - Alkalinity Testing: Proceed with installation if the pH readings are within the specifications given by the adhesive manufacturer.

        - Moisture Testing: If applicable, perform ASTM F2170 relative humidity test and proceed with installation only after substrates are below relative humidity of the selected adhesive.  Or perform ASTM F1869 calcium chloride test and proceed with installation only after substrates are below the maximum moisture-vapor-emission rate of the selected adhesive. Where only one test protocol can be performed, ASTM F2170 is preferred.

        - Use trowelable concrete based leveling and patching compound with the same moisture vapor tolerance as the adhesive to fill depressions, holes, and other irregularities in substrate. For dormant cracks and saw cuts refer to manufacturer’s installation instructions.

        - Place flooring and installation materials into spaces where they will be installed at least 48 hours before installation. Install flooring materials only after they have reached the same temperature as space where they are to be installed.

        - Mechanically prepare the surface of the concrete slab per ASTM F710.

        - Sweep and then vacuum substrate immediately before installation. After cleaning, examine substrate for moisture, alkaline salts, grit, dust or other contamination. Proceed with installation only after unsatisfactory conditions have been corrected.

      - VINYL TILE FLOORING INSTALLATION

        - General:

          - Comply with resilient flooring manufacturer's installation instructions.

          - Take necessary precautions to minimize noise, odors, dust and inconvenience during installation.

          - Fit flooring neatly and tightly to vertical surfaces, equipment anchors, floor outlets, and other interruptions of floor surface.

          - Extend flooring into toe spaces, door reveals, closets, and similar openings unless otherwise indicated.

        - Lay out flooring per manufacturer's recommendations.

        - Adhered Flooring: Attach products to substrates using a grid pattern of adhesive applied to substrate to comply with adhesive and flooring manufacturer instructions.

      - CLEANING AND PROTECTION

        - Perform cleaning 72 hours after completing resilient flooring installation:

          - Remove marks and blemishes from flooring surfaces.

          - Sweep and then vacuum flooring.

          - Damp-mop flooring with pH neutral cleaner to remove soiling.

        - Protect flooring from abrasions, indentations, and other damage from subsequent operations and placement of equipment, during remainder of construction period.

END OF SECTION