CREATION 70 is a synthetic, decorative, and flexible PVC flooring solution, available in planks and tiles with four-sided beveled edges. It features a 0,70mm wear-layer, and a high definition printed decorative film, offering an extensive design variety. The product also includes an acoustic top layer for enhanced walking comfort, along with a resilient core that facilitates easy cutting during installation.

With a total thickness of 2,5mm, CREATION 70 benefits from a crosslinked polyurethane surface treatment (Protecshield™), which ensures easy maintenance and improved resistance to micro-scratches.

CREATION 70 is designed for glue-down installation. It is classified as Bfl-s1 according to EN 13501-1 fire safety standard.

CREATION 70 meets the European usage classification 34-43.

CREATION 70 is free from phthalates (except for recycled content) and is 100% recyclable. Installation offcuts and end-of-life material, under certain conditions, can be collected and recycled through Gerflor’s “Second Life” program. The product contains an average of 20% recycled content and complies with REACH regulations. Its indoor air quality performance is excellent, with TVOC emissions after 28 days (NF EN 16000) below 10 µg/m³, earning an A+ rating - the highest level under health labeling standards, Floorscore®, IAC Gold & M1.

CREATION 70 has an EPD certified by UL.