CREATION 55 CLIC is a decorative, flexible flooring solution, classified in abrasion group T, available in planks and tiles with four-sided beveled edges. It features a 0,55mm wear layer and a 2m high definition printed decorative film, offering maximum design variety.

The product also includes an acoustic top layer for improved walking comfort and easier cutting during installation and a rigid core, which allows installation over existing subfloors, making it suitable for renovation projects.

The total thickness is 5mm.

It benefits from a cross-linked polyurethane surface treatment (Protecshield™), which facilitates maintenance and provides resistance to micro-scratches.

CREATION 55 CLIC is quick and easy to install thanks to its Gerflor Fold Down clic system: vertical locking on the short side and horizontal locking on the long side.

It is classified Bfl-s1 according to the fire standard EN 13501-1.

CREATION 55 CLIC meets the European classification 33-42.

CREATION 55 CLIC is phthalate-free (except for recycled content) and 100% recyclable. Installation offcuts and end-of-life flooring (under certain conditions) can be collected and recycled through the Gerflor “Second Life” program.

It contains an average of 33% recycled content, certified by SCS Global Services.

It complies with REACH regulations.

TVOC emissions at 28 days (NF EN 16000) are < 10 µg/m³, rated A+ (the highest rating), and certified Floorscore® and M1.

CREATION 55 CLIC has an individual Environmental Product Declaration (EPD), verified and certified by UL Certification.