GUIDE SPECIFICATION

096519- Resilient Tile Flooring (LVT)

(Section 096519.23 – Resilient / Solid Vinyl Floor Tile)

Gerflor Creation 55 Resilient Tile Flooring

This is an editable document for preparing project specifications for Gerflor Creation 55 Resilient Tile Flooring.

How to use this Guide Specification:

This is an “edit-out” document with specification language for several project options.              Select appropriate text based on the project requirements and delete (edit-out) all other text.

- Specifier notes are shown in blue like this: Editor Notes

- Locations where language for Project-specific requirements is to be inserted or selected are indicated like this: [insert] or [select text].

- Finally, remove Editor Notes and any unused optional text in the final version of the specification document.

This document contains trademarks owned by Gerflor including Creation 55 and ProtecShield

Gerflor CANADA 1440 Hocquart, Saint -Bruno, QC J3V 6E1 CANADA. Phone: (844) 437-3566.                E-mail: gerflorcanada@gerflor.com. Website: www.gerflorcanada.com  
SECTION 096519.23 – Resilient / Vinyl Tile Flooring

- GENERAL

SUMMARY

Section Includes: Resilient vinyl tile flooring.

ACTION SUBMITTALS

Product Data: For each type of product indicated.

Manufacturer Certifications:

Provide certification that accurately identifies the Original Equipment Manufacturer (OEM) of flooring furnished for this project including manufacturer’s name, address and factory location.

Suppliers of Private-Label flooring for this project must identify themselves as such and fully disclose the OEM information listed above.

All “manufacturer” requirements in these specifications must be complied with by the OEM, including warranties, certifications, qualifications, product data, test results, environmental requirements, performance data, etc.

Provide ISO 9001 certification for the OEM of the specified products.

Provide ISO 14001 certification for the OEM of the specified products.

Provide ISO 50001 certification for the OEM of the specified products.

Shop Drawings: Showing installation details and locations of borders, patterns, locations of any floor inserts and any seams.

Samples:

Manufacturer's color chart for selection of available floors

Product samples:

Samples to be a minimum of 6’’ x 6’’

INFORMATIONAL SUBMITTALS

Qualification Data:

For a qualified resilient flooring Manufacturer.

For a qualified resilient flooring Installer.

CLOSEOUT SUBMITTALS

Submit three copies of the following:

Manufacturer maintenance instructions.

Manufacturer material warranty.

QUALITY ASSURANCE

Manufacturer Qualifications:

ISO 9001 Certified.

ISO 14001 Certified.

ISO 50001	Certified.

At least ten years’ active experience in the manufacture and marketing of commercial resilient flooring.

Installer Qualifications:

At least five years’ experience in the installation of resilient flooring.

Experience on at least five projects of similar size, type, and complexity as this project.

Employer of workers for this Project who are competent in techniques required by manufacturer for resilient flooring installation indicated.

Fire Test Characteristics: As determined by testing identical products according to CAN/ULC, by a qualified testing agency acceptable to authorities having jurisdiction.

DELIVERY, STORAGE, AND HANDLING

Store flooring and installation materials in protected dry spaces, with ambient temperatures maintained within range recommended by manufacturer, but not less than 18°C (65°F) or more than 29°C (85°F).

Stack boxes no higher than 36 inches, with edges flush. Acclimate materials in the installation area for 24 hours.

FIELD CONDITIONS

Product Installation:

Maintain temperatures during installation within range recommended by manufacturer, but not less than 18°C (65°F) in spaces to receive flooring one week before installation, during installation, and one week after installation.

After installation, maintain temperatures within the manufacturer’s recommended range, ensuring they are not less than 18°C (65°F) and not more than 29°C (85°F)

Prohibit traffic during flooring installation and for at least 48 hours after flooring installation.

Install flooring only after all other trades, including painting and overhead work, has been completed.

WARRANTY

Manufacturer warrants that flooring products are free from manufacturing defects.  Refer to product-specific warranty document for additional detail and warranty period.

Material warranty must be direct from the product manufacturer.

Material warranties from separate or third-party insurance providers are not valid.

Material warranties from private label distributors are not valid.

Failures include the following:

Material manufacturing defects.

Warranty Period:

For materials: 12 years from date of Substantial Completion.

ENVIRONMENT AND INDOOR AIR QUALITY

LEED® Documentation:

LEED v4 MR Credit, Building Product Disclosure & Optimization, Sourcing of Raw Materials: For products having recycled content, indicate percentage by weight of post-consumer and pre-consumer recycled content.

LEED v4 MR Credit, Building Product Disclosure & Optimization, Environmental Product Declaration: For products having an industry wide EPD.

LEED v4 EQ Credits: For adhesives and flooring, including a statement of VOC content, FloorScore® certified.

Indoor Air Quality Certification:

Flooring products must be FloorScore® Certified.

FloorScore® certification proves compliance with the volatile organic compound emissions criteria of the California Section 01350 standard.

FloorScore® certification proves compliance with the testing and product requirements of the California Department of Health Services “Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers.”

FloorScore® documentation must include certificate number for specified product.

Manufacturer Certification of Environmental Procedures:

Original Equipment Manufacturers (OEM) ISO 14001 Certification

COORDINATION

Coordinate layout and installation of flooring with other equipment.

- PRODUCTS

COMMERCIAL RESILIENT / VINYL TILE FLOORING

- Editor Note: Select specific Creation 55 Trend and description where indicated.

Basis-of-Design Manufacture: Subject to compliance with requirements, provide Gerflor Creation 55

- Gerflor’s Creation 55 a 2.5mm thick vinyl tile product in plank or tile format with a printed design protected by a 0.55mm thick transparent wearlayer and including the ProtecShield surface treatment.

- Flooring installed with full-spread standard adhesive.

Editor Note:

Select one of the following 3 paragraphs to address consideration of additional manufactures:

If no substitutions will be accepted:

Substitution Limitations:

No substitutions.

If products from other manufacturers will be considered, insert the manufacture’s name and the product name and/or model number:

        - Other Manufactures: Subject to compliance with all the requirements of this specification, provide products by one of the following:

[Insert flooring manufacturer name]: [Insert flooring product name/model].

If other manufacturers are allowed to submit requests for approval prior to bid:

        - Substitution Limitations:

All other manufacturers: Submit formal substitution request prior to bid in accordance with Section 012500 - "Substitution Procedures”.

Approval by Architect of other manufacturers does not relieve Contractor of responsibility to provide products which comply with all requirements of this specification.

Product Description: Resilient / Vinyl Tile flooring as per ASTM F1700 Class III, Type B

Overall Thickness: Not less than 2.5 mm

Wear-Layer Thickness: Not less than 0.55 mm

Max static load limit must meet ASTM F970

Adhesive Method:

Flooring to be adhered to the concrete slab as recommended in the installation instruction to prevent floor from shifting.

Complete adhesive coverage to eliminate the possibility of gaps or space between the slab and flooring material where moisture could accumulate and create an environment conducive to mold growth.

Flooring to be adhered to the concrete slab in all locations eliminating the possibility of waves or wrinkles forming caused by the floor shifting, moving or by rolling loads displacing it.

100% REACH Compliant.

Applied Permanent Finish: Manufacturer's, factory-applied, permanent, UV-cured.

Polyurethane surface treatment ProtectShield

Tile / Plank Size: dependent on specific Creation design selected.

Colour and Pattern:

As selected by Owner from manufacturer's standard colours and patterns.

Performance Criteria:

ASTM F1700 for Solid Vinyl Floor Tile

Provide test certificate to show compliance with ASTM F1700

ACCESSORIES

Trowelable Leveling and Patching Compound: Latex-modified, hydraulic-cement-based formulation approved by the flooring manufacturer.

Adhesive types recommended by flooring manufacturer for substrate and conditions indicated.

Basis-of-Design Product: Gerflor Gerfix TPS+

Coverage Type: Full-spread or full-surface application.

Adhesive Available for 98% RH Slab Moisture Installations.

Gerfix 196

- PART 3 - EXECUTION

- 3.1EXAMINATION

        - Verify the Following:

The area in which the indoor resilient tile flooring will be installed is dry, weather-tight and in compliance with specified requirements.

Permanent heat, lighting and ventilation systems are installed and operable.

Other work, including overhead work, that could cause damage, dirt, dust or otherwise interrupt installation has been completed or suspended.

No foreign materials or objects are present on the substrate and it is clean, porous, and ready for preparation and installation.

Tests to verify that the moisture vapor emission rate or substrate relative humidity is within the specified ranges.

The concrete slab surface pH level is within the specified range, if applicable.

The surface of concrete floors shall be flat to within the equivalent of (3.9mm) 3⁄16" in 3 meters (10 ft) as described in ASTM F710.

The concrete slab complies with ACI 302.2R for concrete design including use of a low-permeance vapor barrier directly beneath the concrete subfloor with sealed penetrations.

PREPARATION

Prepare substrates according to manufacturer's written recommendations to ensure proper adhesion of resilient flooring system.

Concrete Substrates: Prepare according to ASTM F710.

Verify that substrates are dry and free of sealers, curing compounds and other additives. Remove coatings and other substances that are incompatible with adhesives using mechanical methods to create porosity as recommended by manufacturer.

Alkalinity Testing: Proceed with installation if the pH readings are within the specifications given by the adhesive manufacturer.

Moisture Testing: If applicable, perform ASTM F 2170 relative humidity test and proceed with installation only after substrates are below relative humidity of the selected adhesive.  Or perform ASTM F1869 calcium chloride test and proceed with installation only after substrates are below the maximum moisture-vapor-emission rate of the selected adhesive. Where only one test protocol can be performed, ASTM F2170 is preferred.

Use trowelable concrete based leveling and patching compound with the same moisture vapor tolerance as the adhesive to fill depressions, holes, and other irregularities in substrate. For dormant cracks and saw cuts refer to manufacturer’s installation instructions.

Place flooring and installation materials into spaces where they will be installed at least 48 hours before installation. Install flooring materials only after they have reached the same temperature as space where they are to be installed.

Mechanically prepare the surface of the concrete slab per ASTM F710.

Sweep and then vacuum the substrate immediately before installation. After cleaning, examine substrate for moisture, alkaline salts, grit, dust or other contamination. Proceed with installation only after unsatisfactory conditions have been corrected.

VINYL TILE FLOORING INSTALLATION

General:

Comply with resilient tile flooring manufacturer's installation instructions.

Take necessary precautions to minimize noise, odors, dust, and inconvenience during installation.

Fit flooring neatly leaving a ¼" (6 mm) gap to vertical surfaces, equipment anchors, floor outlets, and other interruptions of floor surface.

Extend flooring into toe spaces, door reveals, closets, and similar openings unless otherwise indicated.

Lay out flooring per manufacturer’s recommendations:

Work from center marks established between primary walls so that opposite edges of plank flooring are approximately equal in width.

Lay planks starting at center marks in rooms and corridors.

Arrange planks towards the main window or parallel to the longest wall.

Arrange planks in direction of traffic in corridors.

Cut plank flooring to accommodate vertical surfaces, fixtures, and built-in furniture including cabinets, pipes, outlets, and door frames. Fit plank flooring neatly at equipment anchors, floor outlets, and other interruptions of floor surface.

Leave an expansion gap of ¼" (6mm) at all vertical objects and surface intersections.

Adhered Flooring to substrates to comply with adhesive and flooring manufacturer instructions.

CLEANING AND PROTECTION

Perform cleaning 72 hours after completing resilient flooring installation:

Remove marks from flooring surfaces.

Sweep and then vacuum the flooring.

Damp-mop flooring with pH neutral cleaner to remove soiling.

Protect flooring from abrasions, indentations, and other damage from subsequent operations and placement of equipment, during remainder of construction period.

END OF SECTION