This is an editable document intended to assist in preparing project specifications for Taraflex sports flooring, formatted as a model specification in accordance with Construction Specifications Canada (CSC) standards:

|  | Product Name | Installation method |
| --- | --- | --- |
|  | Taraflex Surface | Full-Spread Installation |
|  | Taraflex BleacherBlok | BleacherBlok SV installed under bleacher area |

How to use this Guide Specification:

This is an “edit-out” document with specification language for several project options.              Select appropriate text based on the project requirements and delete (edit-out) all other text.

- Specifier notes are shown in blue like this: Editor Notes

- Locations where language for Project-specific requirements is to be inserted or selected are indicated like this: [insert] or [select text].

- Finally, remove Editor Notes and any unused optional text in the final version of the specification document.

This document contains trademarks owned by Gerflor including Taraflex, Gerfix 100, Gerflor T-111, Protecsol and BleacherBlok.

Gerflor CANADA, 1440 Hocquart, Saint -Bruno, QC J3V 6E1 CANADA. Phone: (877) 437-3566.                E-mail: gerflorcanada@gerflor.com. Website: www.gerflorcanada.com  
SECTION 096566 - RESILIENT ATHLETIC FLOORING

- GENERAL

SUMMARY

Section Includes: Sheet vinyl resilient athletic flooring.

ACTION SUBMITTALS

Product Data: For each type of product indicated.

Manufacturer Certifications:

Provide certification that accurately identifies the Original Equipment Manufacturer (OEM) of flooring furnished for this project including manufacturer’s name, address and factory location.

Suppliers of Private-Label flooring for this project must identify themselves as such and fully disclose the OEM information listed above.

All “manufacturer” requirements in these specifications must be complied with by the OEM, including warranties, certifications, qualifications, product data, test results, environmental requirements, performance data, etc.

Provide ISO 9001 quality certification for the OEM of the specified products.

Provide ISO 14001 environmental certification for the OEM of the specified products.

Provide ISO 50001 energy certification for the OEM of the specified products.

Laboratory Test Results:

Provide certification of testing in accordance with ASTM F970, demonstrating that the BleacherBlok product furnished is capable of withstanding point loads of up to 750 psi (5.17 MPa) with a residual indentation not exceeding 0.127 mm (0.005 inch).

Fire Test Characteristics: Determined through testing of identical products in accordance with the CAN/ULC-S102.2 standard, performed by a qualified testing agency, including the classification required by local authorities having jurisdiction.

Shop Drawings: Showing installation details and locations of borders, patterns, game lines, locations of floor inserts and seams.

Samples:

Manufacturer's colour chart for selection of available floors with a minimum of 10 standard colours available, including 3 wood visuals.

Colour samples:

Provide wood visual samples measuring a minimum of 610 mm (24 inches) by 914 mm (36 inches) to show that the appearance of wood plank pattern complies with these specifications

Solid colour samples: Minimum 15cm (6 inches) by 20cm (8 inches).

INFORMATIONAL SUBMITTALS

Qualification Data:

For a qualified resilient athletic flooring Manufacturer.

For a qualified resilient athletic flooring Installer.

CLOSEOUT SUBMITTALS

Submit three copies of the following:

Manufacturer maintenance instructions.

Manufacturer material warranty.

Installer installation warranty.

QUALITY ASSURANCE

Manufacturer Qualifications:

ISO 9001 Certified.

ISO 14001 Certified.

At least ten years’ active experience in the manufacture and marketing of indoor resilient athletic flooring.

A provider of authorized installer training.

Installer Qualifications:

At least five years’ experience in the installation of resilient athletic flooring.

Experience on at least five projects of similar size, type and complexity as this project.

Employer of workers for this Project who are competent in techniques required by manufacturer for resilient athletic flooring installation indicated.

DELIVERY, STORAGE, AND HANDLING

Store flooring and installation materials in protected dry spaces, with ambient temperatures maintained within range recommended by manufacturer, but not less than 13° C (55° F) nor more than 29° C (85° F).

Store the indoor resilient athletic surfacing rolls in an upright position on a smooth flat surface immediately upon delivery to Project.

FIELD CONDITIONS

Product Installation:

Maintain temperatures during installation within range recommended by manufacturer, but not less than 18° C (65° F) in spaces to receive flooring for 48 hours prior, during and 48 hours after (2 days) the installation.

After installation, maintain temperatures within the range recommended by manufacturer, but not less than 13° C (55° F) or more than 29° C (85° F).

Prohibit traffic during flooring installation and for at least 48 hours after flooring installation.

Install flooring only after other finishing work, including painting and overhead work, has been completed.

WARRANTY

Special Limited Warranty: Manufacturer's standard form in which manufacturer agrees to repair or replace sports flooring that fails within specified warranty period.

Material warranty must be directed by the product manufacturer.

Material warranties from private label distributors are not valid.

Failures include, but are not limited to, the following:

Material manufacturing defects.

Failure due to substrate moisture exposure not exceeding 95% relative humidity (RH) when tested according to ASTM F2170

Warranty Period: 15 years from date of Substantial Completion.

Special Limited Warranty: Installer's standard form in which installer agrees to repair or replace sports flooring that fails due to poor workmanship or faulty installation within the specified warranty period.

Warranty Period: 1 year from date of Substantial Completion.

ENVIRONMENT AND INDOOR AIR QUALITY

LEED® Documentation:

LEED® v4 MR Credit, Building Product Disclosure & Optimization, Environmental Product Declaration: Provide at minimum a product specific UL certified Environmental Product Declaration (EPD).

LEED® v4 MR Credit, Building Product Disclosure & Optimization, Sourcing of Raw Materials: For products having recycled content, indicate percentage by weight of post-consumer and pre-consumer recycled content.

LEED® v4 EQ Credits: For adhesives and flooring, including a statement of VOC content, FloorScore® certified.

Indoor Air Quality Certification:

Flooring products must be FloorScore® Certified.

FloorScore® certification proves compliance with the volatile organic compound emissions criteria of the California Section 01350 standard.

FloorScore® certification proves compliance with the testing and product requirements of the California Department of Health Services “Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers.”

FloorScore® documentation must include certificate number for specified product.

Manufacturer Certification of Environmental Procedures:

Original Equipment Manufacturers (OEM) ISO 14001 Certification

Manufacturer’s Certification to Inhibit the Spread of Bacteria

Submit documentation confirming that the product is certified compliant with ISO 22196, demonstrating a bacteriostatic treatment capable of inhibiting bacterial growth by 99.9 percent.

COORDINATION

Coordinate layout and installation of flooring with other gymnasium equipment.

- PRODUCTS

SHEET VINYL ATHLETIC FLOORING

Basis-of-Design Manufacturer: Subject to compliance with requirements, provide Gerflor Taraflex Surface Sports Flooring installed with Gerflor full-spread adhesive, with BleacherBlok underlayment beneath bleacher areas.

Editor Note:

Select one of the following 3 paragraphs to address consideration of additional manufactures:

If no substitutions will be accepted:

Substitution Limitations:

No substitutions.

If products from other manufacturers will be considered, insert the manufacture’s name and the product name and/or model number:

        - Other Manufactures: Subject to compliance with all the requirements of this specification including full-spread adhesive coverage provide products by one of the following:

[Insert flooring manufacturer name] : [Insert flooring product name/model].

If other manufacturers are allowed to submit requests for approval prior to bid:

        - Substitution Limitations:

All other manufacturers: Submit formal substitution request prior to bid in accordance with Section 012500 - "Substitution Procedures”.

Approval by Architect of other manufacturers does not relieve Contractor of responsibility to provide products which comply with all requirements of this specification including full-spread adhesive coverage.

Product Description: Dual-durometer foam-backed sheet vinyl flooring designed for fully adhered athletic flooring applications.

Overall Thickness: Not less than 2.1mm (0.08 inches).

Wear-Layer Thickness: Not less than 2.0mm (0.08 inches)

Seaming Method: Heat welded.

Adhesive Method:

Full-spread adhesive coverage to completely adhere flooring to substrate.

Complete adhesive coverage to eliminate the possibility of gaps or space between the slab and flooring material where moisture could accumulate and create an environment conducive to mould growth.

Flooring to be fully adhered to the concrete slab in all locations eliminating the possibility of waves or wrinkles forming caused by the floor shifting, moving or by rolling loads displacing it.

Adhesive shall be resistant to moisture levels up to 100 percent relative humidity (RH) as tested in accordance with ASTM F2170, or a moisture vapor emission rate up to 25 pounds per 1,000 sq. ft. per 24 hours as tested in accordance with ASTM F1869.

Traffic-Surface Texture: Wood visual shall have wood grain embossed texture for a genuine wood appearance and Solid colours to have “pebbled” embossed texture for an attractive appearance.

Applied Finish: Manufacturer's, factory-applied, permanent and UV-cured.

No-Wax finish: Published product literature identifying factory applied finish as, “No-Wax-Just clean and rinse”

Basis-of-Design Product: Gerflor Protecsol.

Field-Applied Finishes: None required and not allowed.

Roll Size:

Roll Width: Rolls to be a minimum width of 1.5m (59 inches) wide.

Roll Length:

Wood visual rolls to be a minimum length of 26.4lm (86’6”) to minimize the number of end-seams.

Solid colour rolls shall be a minimum length of 20.5m (67’3”) to minimize the amount of waste if accent colours are selected for boarders, keys or centre circle.

Roll length of wood visual flooring shall be sufficient to cover the full length of a high school main basketball court 25.6m (84’-0”) without splicing or end-of-roll (butt) seams within main court boundary.

BleacherBlok tile size 152cm (60”) wide x 152cm (60”) long 5mm thick

Colour and Pattern:

As selected by Owner from manufacturer's standard colours and patterns.

Wood pattern shall accurately simulate the true visual appearance of natural athletic wood strip flooring.

Pattern shall replicate random-length stock by simulating non-uniform board lengths ranging from 46cm (18 inches) to 122cm (48 inches) with a maximum board width of 6.4 cm (2-1/2 inches).

Wood pattern shall not include a dark line simulating edges or ends of individual boards.

Surface texture shall simulate realistic wood grain and not be raised or "pebbled" embossing.

Performance Criteria:

ASTM F2772-11 Indoor Sport Floor Standard:

Provide certification of compliance for the four ASTM F2772 Indoor Sport Floor Standard performance categories:

Shock Absorption/Force Reduction:

N/A

Ball Bounce:

Minimum 90%: Pass

Surface effect/Coefficient of Friction:

Between 80-110: Pass

Vertical deformation:

Maximum 3.0 mm (0.14 inches): Pass

Static Load Limit/Residual Indentation:

EN 1516; Pass, Less than or equal to 0.5 mm.

Resistance to Rolling Load: EN1569: Pass

Chemical Resistance: ASTM D543: OK

Abrasion Resistance: EN ISO 5470: Pass

Gloss/Brightness: EN ISO 2813: Pass

Organic Emission: ASTM D5116: Pass

Fire Performance: ASTM E648: Greater than 0.45 W/cm2, Class 1

Slab Moisture Design Tolerance: Maximum relative humidity (RH) of 100% when tested according to ASTM F2170

Surface Maintenance Requirements: No-wax surface requiring only cleaning and rinsing.

Fire Performance: CAN/ULC-S102.2; FSV: 225 SDV: 105

INDENTATION RESISTANT SYSTEM

Editor Note: Location of BleacherBlok should be coordinated on the drawings.

Basis-of-Design Product: Gerflor Taraflex BleacherBlok System for increase durability and up to 750 lb/in² (psi) indentation resistance under the bleachers.

Location: [Under stacking position only of bleachers] or [Under stacking and extended position of bleachers] or [As indicated on drawings]

Performance Criteria: BleacherBlok system capable of withstanding point loads up to 750 lb/in² (psi) per ASTM F970 with less than 0.127mm (0.005-inch) residual indentation

Description: Gerflor Taraflex Surface top layer over a high-density underlayment capable of withstanding loads imposed by bleachers or other heavy equipment.

System: 2.1 mm thick Surface wear layer over a lower layer of dense support underlayment installed at targeted areas in the gym.

Total Surface wear layer: Minimum 2.1mm thick Surface wear layer of identical material, construction, and characteristics as the wear layer of the resilient athletic flooring specified elsewhere in this section.

Lower support underlayment: Dense support layer of appropriate thickness to provide up to 750 lb/in² (psi) load protection under bleachers.

Overall Thickness: The combined thickness of the BleacherBlok system will match the total thickness of resilient athletic flooring installed adjacent to the BleacherBlok.

Adhesive to substrate: Gerfix 100 full-spread adhesive, with the same 100% RH slab moisture tolerance as specified for the adhesive used with adjacent sport flooring.

Adhesive to BleacherBlok: Gerflor T-111 full-spread adhesive, with the same 95% RH slab moisture tolerance as specified for the adhesive used with adjacent sport flooring.

Seaming method: Heat weld top Surface wear layer to match adjacent sport flooring

ACCESSORIES

Adhesive Taraflex Surface sports flooring: High moisture tolerant adhesive recommended by athletic flooring manufacturer for substrate and conditions indicated.

Basis-of-Design Product: Gerflor T-111 (95% RH / 8 lbs)

Coverage Type: Full-spread application for 100% coverage.

Slab Moisture Tolerance: Up to 95% relative humidity (RH) when tested according to ASTM F2170.

Adhesive for BleacherBlok: High moisture tolerant adhesive recommended by athletic flooring manufacturer for substrate and conditions indicated.

Basis-of-Design Product: Gerfix 100 (100% RH / 25 lbs)

Coverage Type: Full-spread application for 100% coverage.

Slab Moisture Tolerance: Up to 100% relative humidity (RH) when tested according to ASTM F2170.

Heat Welding Rod: As supplied by indoor resilient athletic flooring manufacturer. Colour shall blend with resilient athletic flooring colour.

Game-Line and Marker Paint: Complete system including primer, compatible with flooring and recommended by flooring and paint manufacturers.

- EXECUTION

EXAMINATION

Verify the Following:

The area in which the indoor resilient athletic flooring will be installed is dry, weather-tight and in compliance with specified requirements.

Permanent heat, lighting and ventilation systems are installed and operable.

Other work, including overhead work, that could cause damage, dirt, dust or otherwise interrupt installation has been completed or suspended.

No foreign materials or objects are present on the substrate and that it is clean and ready for preparation and installation.

Tests to verify that the moisture vapour emission rate or substrate relative humidity is within the specified ranges.

The concrete slab surface pH level is within the specified range.

The concrete slab surface deviation is no greater than 4.8 mm (3/16 inches) within 3m (10 feet) when measured according to ASTM E1155.

The concrete slab complies with ACI 302.2R for concrete design including use of a low-permeance vapour barrier directly beneath the concrete subfloor with sealed penetrations.

PREPARATION

Prepare substrates according to manufacturer's written recommendations to ensure proper adhesion of resilient athletic flooring system.

Concrete Substrates: Prepare according to ASTM F710.

Verify that substrates are dry and free of sealers, curing compounds and other additives. Remove coatings and other substances that are incompatible with adhesives using mechanical methods recommended by manufacturer.

Alkalinity Testing: Perform pH testing according to ASTM F710. Proceed with installation only if pH readings are between 7.0 and 8.5.

Moisture Testing: Perform ASTM F2170 relative humidity test and proceed with installation only after substrates have maximum relative humidity (RH) of 98%.

Use a trowel-applied, cementitious leveling and patching compound with moisture tolerance equivalent to that of the specified adhesive, to fill depressions, voids, and surface irregularities in the substrate. Address dormant cracks and saw cuts in accordance with the flooring manufacturer's written installation instructions.

Place flooring and installation materials into spaces where they will be installed at least 48 hours before installation. Install flooring materials only after they have reached the same temperature as space where they are to be installed.

Sand the surface of the concrete slab.

Sweep and then vacuum substrates immediately before installation. After cleaning, examine substrate for moisture, alkaline salts, grit, dust or other contamination. Proceed with installation only after unsatisfactory conditions have been corrected.

SHEET ATHLETIC FLOORING INSTALLATION

General:

Comply with resilient athletic flooring manufacturer's installation instructions.

Take necessary precautions to minimize noise, odours, dust and inconvenience during installation.

Fit flooring neatly and tightly to vertical surfaces, equipment anchors, floor outlets, and other interruptions of floor surface.

Extend flooring into toe spaces, door reveals, closets, and similar openings unless otherwise indicated.

Lay out flooring as follows:

Minimize the number of seams and place them inconspicuous areas.

Locate seams as shown on approved shop drawings.

Adhered Flooring: Attach products to substrates using a full-spread of adhesive applied to substrate to comply with adhesive and flooring manufacturer instructions.

Vinyl Sheet Flooring Seams: Finish seams to produce surfaces flush with adjoining flooring surfaces. Comply with ASTM F1516 for heat welded seams. Rout joints and use heat welding rod to permanently and seamlessly fuse sections together.

GAME LINES AND LOGOS

Lay out game lines and logos in accordance with the official rules and diagrams published by the relevant Canadian national sport governing bodies for each sport, unless otherwise specified by local authority having jurisdiction.

Mask flooring at game lines and logos, and apply paint of colour indicated to produce clean, sharp and distinct edges.

CLEANING AND PROTECTION

Perform the following operations after completing resilient athletic flooring installation:

Remove marks and blemishes from flooring surfaces.

Sweep and then vacuum the flooring.

Damp-mop flooring to remove soiling.

Protect flooring from abrasions, indentations, and other damage from subsequent operations and placement of equipment, during remainder of construction period.

END OF SECTION