[image: image1.png]Gerflor





ATTRACTION CLEANTECH

ATTRACTION CLEANTECH is a multi-layered, loose-lay vinyl tile with a thickness of 5 mm, reinforced by two glass fiber grids. These tiles are available in a square format with welded joints, making them ideal for clean environments and watertight system requirements.
ATTRACTION CLEANTECH features a 1 mm homogeneous vinyl wear layer, manufactured through a continuous high-pressure process offering exceptional resistance to heavy traffic and static loads (UPEC classification U4P4).

ATTRACTION CLEANTECH is treated with Protecsol®2 surface treatment, ensuring easy maintenance and eliminates permanently the need for acrylic emulsion (metallization). It avoids staining of chemical products used in healthcare like iodine alcohol, Betadine, eosin and anti-bacterial hand gel.
ATTRACTION CLEANTECH has a Bfl-s1 fire classification in accordance with standard EN 13501-1.
ATTRACTION CLEANTECH is non-emissive of volatile organic compounds, with levels <10 μg/m³ (TVOC after 28 days, ISO 16000-6).

Product Description

gerflor.com

[image: image1.png]