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GTI MAX

GTI MAX neoCONNECT is a multi-layered loose-lay vinyl tile with a total thickness of 6 mm, reinforced by two glass fibre grids. The tiles are installed using an interlocking dovetail system and are recommended in brick bond installation to improve layout stability and visual alignment in high traffic areas.

GTI MAX CLEANTECH is the watertight version of GTI MAX. It is a multi-layered loose-lay vinyl tile with a total thickness of 6 mm, reinforced by two glass fibre grids, supplied in square format with welded joints for clean environments and areas requiring watertightness.

GTI MAX features a 2 mm homogeneous vinyl wear layer, manufactured through a continuous high-pressure process, providing resistance to heavy traffic and static loads. The product achieves UPEC classification U4P4S.

GTI MAX is treated with a Polyurethane (PUR) surface treatment, ensuring easy maintenance and helping to prevent staining from various chemicals used in industrial environments. The surface treatment requires no waxing throughout the product’s lifespan.

GTI MAX has permanent antistatic properties: <2000V according to EN1815.

GTI MAX is non-emissive of volatile organic compounds, with levels <10 μg/m³ TVOC after 28 days, according to ISO 16000-6.
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